ORDER DESCRIPTION

- Object of the contract

The subject of the contract is metals for evaporation of increased purity in the amount of:

- Nickel 4.5N 								100 g

- Platinum 4N 								100 g

- Palladium 4N 								20 g

- Gold-Germanium 4N							100 g

- The scope of the subject of the contract

A detailed description of the subject of the contract is provided in section 5 of this document. The total price for the products specified in point 1 should include the total cost along with the packaging and delivery to the headquarters of the Employer.

- Criterion

Offers will be evaluated according to a point scale with a maximum number of points of 100.

| Criterion | Maximum number of points S | Method of awarding points |
| --- | --- | --- |
| Price (P) | 100 | S x Pmin/Pi |

Where:

- Pi – price of goods with delivery - for the given offer

- Pmin - the minimum delivery price for the ordered goods from all offers submitted

- S – number of points

The final score will be calculated by adding up the partial components and then rounded to two decimal places (rounded from "5" up).

- Deadline for completing the order

As soon as possible, no later than 4 weeks from the date of placing the order.

Deadline for completion of the order includes readiness to hand over the goods to the Ordering Party, which complies with application of the DAP Incoterms2020 principle.

According to the DAP (delivery at place) principle, the moment of delivery of the goods is deemed to be to the place - the headquarters of the Contracting Party.

The Ordering Party shall accept application of other Incoterms2020 principle (such as FCA, DAP etc.), on condition that the Contractor will meet the deadline for completion, as referred to above.

- Parameters

5.1 Detailed scope of the subject

- Part I

| Product name | Parameter | Specification |
| --- | --- | --- |
| Nickel | Purity | ≥99,995% |
|  | Dimensions | Pellets with dimensions: diameter ⅛” length ⅛” |
|  | Impurities | Ag ≤ 0.05 ppm Co ≤ 1,6 ppm C ≤ 12 ppm Cr ≤ 2,7 ppm |

- Part II

| Product name | Parameter | Specification |
| --- | --- | --- |
| Platinum | Purity | ≥99,99% |
|  | Dimensions | Pellets with dimensions: diameter ⅛” length ⅛” |
|  | Impurities | Ag ≤ 13 ppm Al ≤ 2 ppm Cu ≤ 2 ppm Si ≤ 17 ppm Zn ≤ 5 ppm |

- Part III

| Product name | Parameter | Specification |
| --- | --- | --- |
| Palladium | Purity | ≥99,99% |
|  | Dimensions | Shots with dimensions: diameter ⅛” length ⅛” |
|  | Impurities | Ir ≤ 6 ppm Fe ≤ 2 ppm Rh ≤ 1 ppm |

- Part IV

| Product name | Parameter | Specification |
| --- | --- | --- |
| Gold-Germanium | Purity | ≥99,99% |
|  | Dimensions | Pellets with dimensions: diameter ⅛” length ⅛” |
|  | Impurities | Ag ≤ 2,7 ppm Fe ≤ 1,7 ppm Si ≤ 1,6 ppm |